In vitro intestinal toxicity of commercially available spray disinfectant products advertised to contain colloidal silver

Table 1. Consumer product silver concentration Total Claimed, Total Measured and Soluble (Filtrate)

_____________________________________________________________________________

Product		Total Ag Claimed	Total Ag Measured 	Filtrate (soluble Ag)

(mg/L)			(mg/L)			(mg/L)

_____________________________________________________________________________

1		120			18.9 ± 0.9		18.6 ± 0.5

2		500			960.8 ± 28.6		4.9 ± 0.1

3		NR			6.0 ± 1.1		BDL

4		NR			6.1± 0.1			BDL

5		NR			8.7 ± 0.7		0.2 ± 0.1

_____________________________________________________________________________

NR Not Reported

BDL Below Detection Limit

Table 2. Hydrodynamic diameter, primary particle size for selected products

before and after treatment with Synthetic Stomach Fluid (SSF).

_____________________________________________________________________________________

Hydrodynamic Diameter							 TEM Particle Diameter

_____________________________________________________________________________________

Product		NTA Mean (nm)		DLS_Z-AVG (nm)	PDI		P-1 (nm)	P-2 (nm)

_____________________________________________________________________________________

1		184 ± 125		166 ± 31		0.43		2.3		30-200

1+ SSF		232 ± 57 		180 ± 29		0.33		ND		ND

2		77 ± 38	 		47 ± 0.6			0.48		4.5		20-40

2+ SSF		278 ± 120		715 ± 65 		0.23		ND		ND

3		199 ± 209	 	245 ± 11		0.29		15.5		15-30

3 + SSF		132 ± 180		ND			ND		ND		ND

4		222 ± 177 		220 ± 5.8		0.34		5.2		15-30

4 + SSF		63 ± 48			ND			ND		ND		ND

5		200 ± 72		421 ± 40		0.43		ND		20-50

5 + SSF		311 ± 130		ND			ND		ND		ND

ND Not Determined

Table 3. Suggested Cause for Cellular Response

_____________________________________________________________________________

Product		Soluble Ag Sufficient	Particulate Ag Sufficient 	Unexplained Response

to Cause Cell		to Cause Cell			Contribution from Product

Response		Response			Matrix

(mg/L after 1:5) 	(mg/L after 1:5)			(mg/L after 1:5)

_____________________________________________________________________________

1		Yes (3.7)		No (1.6)				No

2		No (1.0)			Yes (191)			No

3		No (BDL)		No (1.2)				Yes

4		No (BDL)		No (1.2)				Yes

5		No (BDL)		No (4.3)				Yes

_____________________________________________________________________________

BDL Below Detection Limit

Fig. 1

Table S-1. Characteristics of Colloidal Silver Product Suspensions

____________________________________________________________

Product		pH			Cl- (ppm)		S (ppm)

____________________________________________________________

1		6.6			BDL			27.9

2		7.9			39.8			40.4

3		10.6			25.1			BDL

4		10.0			25.3			BDL

5		2.5			10.6			9.8

____________________________________________________________

BDL Below Detection Limit

Table S-2. Estimated Total Ag Doses from Recommended Product Use

Product		Product Application 	Total Measured Ag	Recommended Dose	Dose/Day			(External, Internal)	(mg/L)			(mL)			(ug Ag)

___________________________________________________________________________________

1		Internal			18.9			0.4			7.6

2		Both			961			1			961

3		External		6.0			Light Spray		ND

4		External		6.1			Light Spray		ND

5		External		8.7			Hard Surface Spray	ND

___________________________________________________________________________________

ND Not Determined

Fig. S-1